Homework #2: Assigned on 9/17, Due on 9/27 before class.

(Use lecture slides as well as assigned readings (Ratner, Callister, and Black) to answer the questions)

- (30 points) Please review lecture slides and supplemental reading from chapters 4 and 7.8 of the Biomaterials Science text by Ratner et al. Using your own words, answer the following questions as concisely as possible.

  - What is the purpose and sequence of inflammation? Be concise!

6 pts total

(2 pts) Purpose: contain and neutralize the injury (initialize healing)

(4 pts  +2 pts for all steps included, +2 pts for correct order) Sequence:

- activation of coagulation factors,

- increased blood flow,

- infiltration of immune cells,

- leads to chronic inflammation and wound healing (remodeling)

Acute Inflammation  Chronic Inflammation  Granulation/Tissue Remodeling

If give above answer simplified without details included instead just give 3 points

  - What are fibrous capsules and how may they contribute to atrophy around an implant?

6 points total

(3 pts) Fibrous capsules are acellular, collagen-dense capsules that “wall off” (isolate) foreign bodies

(2 pts) They limit blood supply/nutrition

  - Why are implants often hosts for infection?

6 points total

Foreign body, bacterial adhesion, surgery = intrinsic risks for introducing infection, fibrous capsules block immune cell access to infection

4 examples mentioned: Full credit (6 pts)

3 examples: 5 pts

2 examples: 4 pts

1 examples: 3 pts

  - What are cytokines and what are their most prominent activities?

6 points total

(3 pts) Description of cytokines & role in the immune system response

(3 pts) Provides examples of cells that release cytokines and their functions (Macrophages – initiate inflammatory immune response, neutrophils – IL-8 to attract more neutrophils, cytokines are also released by epithelial cells that lead to vasodilation, cytokines released by T-helper cells, etc.)

  - What is the purpose of blood coagulation, and how may this be problematic in the context of blood-materials interactions?

6 points total

(3 pts) Forms fibrin clot to prevent blood loss and localize inflammatory response

(3 pts) Exaggerated immune response, thrombosis/embolism, improper mechanical fixation and function of the implant

- (25 points) Assume that a metal with a BCC structure has atom contact along the body diagonal.

- Derive the relationship between the axial length (a) and the radius of the metal ion (R)

5 points total

(3 pts) Correct formulas

(2 pts) Correct final relationship

Let a be the axial length and let b be the distance of the diagonal of a face. Then from the Pythagorean theorem:

a2+a2=b2
2a2=b2
b=2*a

The body diagonal, d, is equal to 4R:

d=4R

Define d using the Pythagorean theorem:

a2+b2=d2

Substituting b and d:
a2+2*a2=4R2
a2+2a2=16R2
3a2=16R2
a=43*R=4R33

- Show that the atomic packing factor of a BCC metal is 0.68

10 points total

(7 pts) Correct formulas

(3 pts) Correct numbers

APF=volume of atoms in a unit cellunit cell volume

Let VA be the volume of atoms in a unit cell and VU be the volume of the unit cell.

First, find the number of atoms in a unit cell. Since it is a BCC structure:

Number of atoms=8×18+1=2

Take the volume of 1 atom to be the volume of a sphere (4/3r3). Thus, the volume of 2 atoms (assuming radius of unit cell is the radius of an atom R) is:

VA=243πR3

From part a, we know the relationship between a and R. Substituting in:

VA=243πa343=π38a3

VU is simply the volume of a cube with sides of length a:

VU=a3

Thus:

APF=VAVU=π38a3a3=π38≈0.68 ∎

- Calculate the density for Chromium, a BCC metal with an ionic radius of 0.063 nm.

10 points total

(5 pts) Correct formulas

(5 pts) Correct numbers

(-2 pts) Using ionic radius instead of atomic radius

Recall formula for theoretical density:

Since Chromium is a BCC metal, n=2.

Look up the atomic weight: ACr=51.9 g/mol.

Avogadro’s number NA = 6.023*1023 atoms/mol

Calculate the volume of the unit cell:

VC=a3=4R333

In this formula, R = atomic radius, not ionic radius! (Take 2 pts off for using ionic radius)

Look up the atomic radius of chromium: RCr=128pm=1.28*10-10 m

Thus:

VC=4*1.28*10-10 m*333

Plugging everything into the equation:

ρ=nAVCNA=2 atoms×51.9gmol4*1.28*10-10 m*333×6.022×1023atomsmol =6.67gcm3

Note: if students used ionic radius instead, they should have the following calculations:

ρ=nAVCNA=2 atoms×51.9gmol4*0.063*10-9 m*333×6.022×1023atomsmol =56.1gcm3

- (25 points) Stainless steel is one of the most common types of material used inside and outside of the body.

- What is the elemental composition of AISI 316L?

7 points total

(1 pt) Mention any trace element

(6 pts) 1 pt for each non-trace element mentioned

60-65% Fe, 17-20% Cr, 12-14% Ni, 2-3% Mo, 2% Mg, <0.03% C

Trace elements: Cu, N, P, Si, S, Mn

- Explain the function of the major alloying elements: Cr, Ni and Mo

6 points total

(2 pts) Cr – forms passivation oxide layer, Cr2O3, which helps to prevent corrosion (also stabilizes BCC form of SSL – α ferrite)

(2 pts) Ni – increases corrosion resistance (also stabilizes FCC form of SSL – γ austenite)

(2 pts) Mo – prevents pitting corrosion, especially in Cl- containing solutions (also stabilizes BCC form)

- Calculate the %cold work (%change in area) of a stainless steel rod with an initial diameter of 0.07 m and a length of 0.18 m.  The final diameter of the rod was 0.05 m and the cold worked length was 0.30 m.

6 points total

%CW=A0-AdA0×100

A0=πr2=π0.035 m2=0.001255π m

Ad=πr2=π0.025 m2=0.000625π m

%CW=0.001225π m-0.000625π m0.00125π m×100=0.00060.001225×100=48.98%

(3 pts) Correct formula

(3 pts) Correct numbers

- What other treatment is needed after cold work to relieve internal stresses?

6 points total

Annealing (Recovery, Recrystallization, and Grain Growth)

| Stress (MPa) | Strain (%) |
| --- | --- |
| 98 150 260 300 450 600 680 780 840 850 855 710 Failure | 0.06 0.10 0.17 0.20 0.30 0.40 0.50 0.60 0.70 0.80 0.90 1.00 |

- (20 points) The following tensile testing data was obtained for an unknown specimen:

- Plot the stress-strain curve, and clearly label the elastic and plastic deformation regions.

5 points total

(1 pt) Correct slope

(1 pt) Correct intercept

(1 pt) Plotted correctly

(1 pt) Elastic region marked

(1 pt) Plastic deformation region marked

Note: mark if plot has incorrect units for strain (should be unitless), but don’t deduct points unless the values are wrong.

Elastic

Plastic

- Determine the modulus of elasticity, yield strength, ultimate tensile strength, fracture strength, and ductility.

10 points total

(2 pts) Modulus of Elasticity (slope of linear region of stress-strain curve): 148.34 GPa

Defined elastic region up to the point (0.40, 600), plastic region after

In Excel, found slope and intercept of the linear region to get y = mx + b

y = 148338.5 x + 5.572703

(2 pts) Yield Strength (intersection of stress-strain curve with 0.2% offset): ~847 MPa (845-850)

0.2% offset is the line with the same slope which passes through (0.002, 0). Slope is 148338.5.

(y-y1)=148338.5(x-x1)

y=148338.5x-148338.5(0.002)+0

Therefore, the equation for 0.2% offset is y = 148338.5 x – 296.677

Plug the strain values from the table above into the offset equation and plot the resulting stress. Estimate the point of intersection from the graph.

(2 pts) Ultimate Tensile Strength (max on stress-strain curve): 855 MPa

(2 pts) Fracture Strength (stress at which failure occurs): 710 MPa

(2 pts) Ductility (strain at which failure occurs): 1%

-1 pt for wrong unit

- From your answers to parts a and b, decide whether this sample is likely based on a metal, ceramic or polymer.  Justify your choice.

5 points total

(3 pts) Correct answer

(2 pts) Correct justification

Metal: Ductile with elastic AND plastic deformation (so it is not a ceramic), but high stress values (so it is not a polymer)

5. (50 points) Compare and contrast the following biomaterials in terms of 1) composition, 2) mechanical properties (E, yield strength, ductility, fracture toughness), and 3) biocompatibility.  To do this, make a comparison table and be concise.

- Ti-6Al-4V

- Hydroxyapatite

- Ultra high molecular weight polyethylene (UHMWPE)

Answers (give credit for similar, or variants with explanations/sources cited):

|  | Ti-6Al-4V | Hydroxyapatite | UHMWPE |
| --- | --- | --- | --- |
| Composition (10 pts, 4 for alloy and, 2 for HA, 2 for UHMWPE, 2 for 45S5 bioactive glass) | 88.3-90.8% Ti 5.5-6.5% Al 3.5-4.5% V Trace: 0.05% N 0.08% C 0.13% O (slides) | Ca10(PO4)6(OH)2 Nano-scale hexagonal platelets Ca/P = 1.67 E Not required, but correct: Trace Elements (PPM): Al 600 Cu 1 Fe 1000 Ge 100 Mg 2000 Mn 300 Na 3000 Pb 4 Si 500 Ti 30 | With n>100,000 MW = 4 * 106 g/mol (0.5 pt for structure, 1.5 pt for n OR molecular weight) |
| E (8 pts, 2 per material) | 110 GPa (slides) 116 GPa (Ratner) | 40-120 GPa (9.2 GPa at body temp) | 0.69 GPa (Callister) 0.5-1.3 GPa (Ratner) |
| Yield Strength (8 pts, 2 per material) | 877 MPa (Callister) 897-1034 MPa (Ratner) | Estimate with ultimate tensile strength 40-100 MPa | 21.4-27.6 MPa (Callister) 20-30 (Ratner) |
| Ductility (8 pts, 2 per material) | 14% EL in 50 mm (Callister) 8% (Ratner) | 2-4% 0.2% or very low | 350-525% (Callister) 130-500% (Ratner) |
| Fracture Toughness (8 pts, 2 per material) | 100 MPa*sqrt(m) | 1 MPa*sqrt(m) | 1.72-5.16 MPa*sqrt(m) |
| Biocompatibility (8 pts, 2 per material) | Excellent for direct contact with tissue/bone, but can have poor surface wear properties if not treated (oxidized) or if in contact with another metal | Excellent for osteoinductive applications, but can lead to excessive exudate and accumulation of trace elements due to ceramic degradation | Biocompatible in joint surface applications, such as the lining of the acetabular cup, where UHMWPE can contact metals Possible wear damage, inflammatory degradation products |

Note: Ti-6Al-4V mechanical properties vary with heat treatment, and HA mechanical properties vary depending on formation temperature and porosity